Technical Specifications

| Property | Value |
| --- | --- |
| Polymer | LDPE containing micronized surface modified Zeolites |
| Form | Pellets |
| Colour | Off White |
| Odour | Odourless |
| Particle Size | 2-3 mm |
| Bulk Denisty | 550 kg/m3 |
| Solubility | Insoluble |
| MFI | 1-2 |
| Stability | Stable at PE processing conditions |

# Packaging Available

25 kg bags

# Safety Information

ROT NOT  MB  doesnot contain Lead (Pb), Mercury (Hg), Cadmium (Cd), Hexavalent Chromium (Cr6), Polybrominated biphenyls (PBB), or Polybrominated di-phenylether complying with the re-stricted substances listed in Article 4(1) of the RoHS Directive.

Disclaimer: This Data sheet and information it contains is considered to be accurate at the date of printing. No representation or warranty, expressed or implied is made as to the accuracy or completeness of the data and information contained in this publication. The seller does not undertake any responsibility for consequential liabilities or damages arising due to the use of the products or their performance. It is the User’s obligation to evaluate and use products safely and within the scope advised in the data sheet and to comply with all applicable laws and regulations.

# Text boxes

Technical Datasheet

ROT-NOT Masterbatch

ROT-NOT MB 3131

ROT-NOT

Testing & Certifications:

# FDA compliant with FDA 21 CFR 177.1520 Clause (a) (1) (i)

Application:

# Add 6-7.5% of MB in PE

- Process at the same processing conditions recommended for the base polymer

- Compatible with LLDPE/LDPE/HDPE/HMDPE

- May cause negligible drop in transparency and gloss

Features:

# Easily processable with Polyethylenes

- FDA Compliant (SGS Report)

- Natural Additives

- Effective at low addition levels of 6-7.5%

- Human Safe

- Ecologically Safe

- Recyclable with the polymers

Product Description:

ROT-NOT Master batch can be used to produce plastic bags and containers with special properties of shelf life enhancement of fresh fruits and vegetables from 40% to 500%.

Fresh Vegetables and Fruits start to ripen after harvesting and during the ripening process, the fruits and vegetables release ethylene gas. This ethylene gas when in the package increases the ripening rate of the fresh produce hence aggravating the ripening process resulting into faster rotting of the fresh produce.  They ethylene gas produced works as a auto catalyst for ripening which in turn produces higher sugar levels causing microbial spoilage of the fruits.

The plastic articles produced by using ROT-NOT MB absorb the harmful ethylene gas produced hence slowing the ripening and rotting process and increasing the shelf life of the packed produce.

The film produces shows upto 5 times increase in the shelf life of Bananas kept without packaging and improves the shelf life of Tomatoes by upto 3 times.

Tests performed on the Tomatoes show that the tomatoes kept in open started to rot in 5 days where as the ones in the ROT-NOT bags were good even on the 10th day compared to the ones in generic plastic bag which developed black spots and mouldy on the 6th day.